### #4, 03/05/04	#4-1

# Definitions of symbols in “Polymer Physics” by Rubinstein & Colby

| symbol | name | defined as | equal to | proviso |
| --- | --- | --- | --- | --- |
| M | molecular weight | mass of one mole of polymerr | M = MoN | end groups’ contribution neglected |
| Mo | monomer molecular weight | mass of one mole of repeating units in a polymer chain |  | primary structure specified |
| N | degree of polymerization | number of repeating units in a polymer chain |  | end groups not counted |
| ( |  | numerical approximation |  |  |
| ( |  | proportional with dimensionless const |  |  |
| ( |  | proportional with dimensional const |  |  |
| r | linear dimension | a measure of size of an object |  |  |
| m | mass | a mass of an object |  |  |
| D | fractal dimension | exponent of linear dimension’s proportionality to mass | m ( rD , m1 = Cmm2 r1 = Cr r2 D = logCm/logCr |  |
| c | polymer mass concentration | mass of polymers of all sizes per unit volume of solution |  |  |
| cN | mass concentration of N-mer | mass of N-mer per unit volume of solution |  |  |
| ( | volume fraction | fraction of occupied volume of polymers per unit volume of solution | ( = c /( | polymer density in bulk is the same as in solution |
| ( | polymer density | density of polymer in bulk state |  |  |
| vm | molar volume of monomer | volume of one mole of repeating unit | vm = Mo/( |  |
| vo | monomer molecular volume | volume of a repeating unit | vo = vm / NAV |  |
| V | pervaded volume | volume of solution spanned by a polymer chain in solution |  |  |

### #4, 03/05/04	#4-2

| (* | overlap volume fraction | volume fraction of occupied volume of a polymer chain in a pervaded volume | (* = N vo / V |  |
| --- | --- | --- | --- | --- |
| P | overlap parameter | ratio of actual volume fraction to overlap volume fraction | P = (V / N vo |  |
| nN XN | mole fraction of polymer with dp equals N, or mole fraction of N-mer | number of moles of N-mer relative to number of moles of polymers of all sizes. |  |  |
| wN | weight fraction of N-mer | mass of N-mer relative to the total mass of polymers of all sizes |  |  |
| zN | z-fraction of N-mer |  |  |  |
| “C” | molar concentration of polymer | total number of moles of polymers of all sizes per unit volume of solution |  |  |
| “CN”* | molar concentration of N-mer | number of moles of N-mer per unit volume of solution |  |  |
| “(n” | number density of polymer | total number of molecules of all sizes |  |  |

### #4, 03/05/04	#4-3

| Mn | number average molecular weight |  |  |  |
| --- | --- | --- | --- | --- |
| Mw | weight average molecular weight |  |  |  |
| Mz | z-average molecular weight |  |  |  |
| p | extent of reaction of polycondensation, MPD |  | p ( 1 |  |
| nN | mole fraction of N-mer at p for polycondensation |  | nN = (1-p)pN-1 |  |